## Slide 1: Extrusion of Ionic Liquid Rayon
R. Hunter Bray
rhb0004@uah.edu
Reliability and Failure Analysis Lab
http://rfal.uah.edu

## Slide 2
Ionic Liquid Rayon
What is Ionic Liquid Rayon?
  Smaller-than-hair, cellulose based fiber currently in development
  Created by dissolving cellulose in IL and extruding the mixture into a coagulation bath
  Has many potential uses including clothing and carbon fiber precursor
  Our goal: develop this process to match current industrial rayon processes.
Notes: Talk about pictures; walk through extrusion

## Slide 3
Ionic Liquids
What are Ionic Liquids?
  Organic compounds that are ionic and behave as a molten salt at temperatures under 100 deg. C.
  Act as organic solvents
  Almost nonexistent vapor pressure; can be dissolve in solutions and recovered

## Slide 4
Making the Mixture
The Process:
  Dry the Ionic Liquid and cellulose
  Weigh dried Ionic Liquid to determine the amount of dry cellulose needed
  Slowly add in cellulose while applying heat and mixing

## Slide 5
Early Mixing Methods
Hot Plate Method:
How it works:
  Magnetic stir bar inside bottle used to mix IL and cellulose
  Heated with plate from the bottom
Issues:
  Mixing takes a very long time
  Shear throughout mixture for mixing is difficult to achieve with stir bar
  Temperature difference between plate and mix is significant
  Cellulose may get burned
  Mixture may take days to achieve
Oil Bath Method:
How it works:
  Mixture is heated from the bottom and sides with an oil bath
  Electric motor turns an impeller for mixing
Issues:
  Mixing still takes a long time
Advantages over the hot plate:
  Faster heating time
  Higher shear for mixing is achieved

## Slide 6
Current Mixing Methods:
Industrial Microwave:
How it works:
  Mixture is heated in intervals using microwaves
  Electric motor turns an glass impeller for mixing
Issues:
  If heating isn’t carefully monitored cellulose will burn
  Care must be taken with glass impeller due to cost
Advantages over other methods:
  Mixing generally takes < 1 day

## Slide 7
Extrusion Process
Basic Idea:
  A mixture is heated to reduce its viscosity
  The hot mixture is forced through a hole into a coagulation medium
  The mixture exits the hole/holes and enters the coagulation bath.
    Causes the IL to dissipate into the coagulation and the cellulose to precipitate into a fiber

## Slide 8
First Extrusions:
How the extrusions were done:
  Hypodermic needle with tips ground flat
  Coagulation medium was heated water in a beaker
  Fibers were extruded by hand into these beakers and then were collected and dried
  Made fibers no more than around a couple feet long
  Lessons learned:
  #1 that we could successfully created fibers using this method
  Learned the importance of wash time
  Observed shrinking of fibers as they dried
Hypodermic Needles

## Slide 9
First Evolution
Process:
  2-ton hydraulic press was outfitted with a custom extrusion head made using needles
  Heated water was placed into coagulation tank where the fibers were extruded
  Increased length of fibers to around 20 feet
  Lessons learned:
  Multiple fibers spun stuck together
  Observed that when fibers dried on a surface, a flat spot would develop
Hydraulic Press

## Slide 10
Current Extrusions:
How the extrusions are done:
  Bottle of mixture is loaded into a pressure vessel
  Mixture is forced through a spinnerette head into a coagulation bath
  Fibers receive additional washing in additional baths
  Three main sections of the extrusion line:
  Pressure vessel assembly and spinnerette
  Coagulation and wash baths
  Drying and Collection
Wet spinning

## Slide 11
Pressure Vessel & Spinneret
Pressure vessel:
  Uses pressure to force the mixture to the spinneret
  Line is heated to reduce the viscosity of the mixture
  Gear pump is an option if higher pressures are desired
  Spinneret:
  Fits into an assembly attached to the pressure vessel
  Contains hair sized and smaller holes for the mixture to enter the coagulation
  Hole size affects fiber size more than anything

## Slide 12
Coagulation and Wash Baths
Coagulation:
  Bath where fibers are precipitated
  Heated bath of either water or alcohol
  Most of Ionic Liquid is washed out in this bath
  Wash Baths:
  Baths that provide additional washing
  Rollers pull fibers through baths and keep fibers under tension
  Heated baths of either water or alcohol
  Should wash out most of remaining Ionic liquid

## Slide 13
Drying and Collecting
Dryer:
  Uses hot, slow moving air to dry the fibers
  Fan is occasionally added to improve drying
  Very important, fibers drying on collector may stick together
  Collector:
  Simple spooling mechanism used to collect fibers

## Slide 14
Post Extrusion Verification
Each extrusion’s variables differ:
  Issues with extrusion can be present
  Fibers in a tow sticking together
  Unusual geometry of fiber
  Fibers containing excess IL after collected
  Issues with the fiber due to mixture problems
Tests to analyze and verify fibers
  Physical observation
  Tensile testing
  Purity testing
  Microscopy
  Comparisons to industrial rayon

## Slide 15
Recap
Making of mixtures:
  Has gone through three evolutions reducing time required for mixing
  Extruding:
  Also has experienced three evolutions
  Fibers are made by extruding a mixture of IL and cellulose into a coagulant
  Has moved from 6” to thousands of meters of fiber
  Requires verification because each extrusion is usually different and various problems can appear in the fibers

## Slide 16: Questions?
UAHuntsville
R. Hunter Bray
RFAL
Rfal.uah.edu
rhb0004@uah.edu